SUGGESTED CANADIAN SPECIFICATIONS

SECTION 10 26 00

C/S Acrovyn® Model BCR-64

Part 1 - General

- Summary

  - This section includes the following types of wall protection systems:

    - Crash Rails

  - Related sections: The following sections contain requirements related to this section:

    - Handrails, Bumper Guards, Corner Guards, Accent Rails, Wall Covering, Wall Panels, Door Protection; refer to section 10 26 00 “Wall and Door Protection”

    - Blocking in walls for fasteners; refer to section 09 22 00 “Supports for Plaster and Gypsum Board”

- References

  - National Building Code of Canada (NBC 2010)

  - National codes (IBC, UBC, SBCCI, BOCA and Life Safety)

  - American Society for Testing and Materials (ASTM)

  - Underwriters Laboratories (UL)

- Submittals

  - General: Submit the following in accordance with conditions of contract and Division 1 specification section 01 33 00 “Submittal Procedures”.

  - Product data and detailed specifications for each system component and installation accessory required, including installation methods for each type of substrate.

  - Shop drawings showing locations, extent and installation details of crash rails. Show methods of attachment to adjoining construction.

  - Samples for verification purposes: Submit the following samples, as proposed for this work, for verification of color, texture, pattern and end cap attachment and alignment.

    - 12" (304.8mm) long sample of each model specified including end cap and mounting hardware.

  - Product test reports from a qualified independent testing laboratory showing compliance of each component with requirements indicated.

  - Maintenance data for wall protection system components for inclusion in the operating and maintenance manuals specified in Division 1.

- Quality Assurance

  - Installer qualifications: Engage an installer who has no less than 3 years experience in installation of systems similar in complexity to those required for this project.

  - Manufacturer’s qualifications: Not less than 5 years experience in the production of specified products and a record of successful in-service performance.

  - Code compliance: Assemblies should conform to all applicable codes including NBC 2010, IBC, UBC, SBCCI, BOCA and Life Safety.

  - Fire performance characteristics: Provide engineered PETG wall protection system components tested to Canadian Required CAN/ULC S102.2, “Test for Surface Burning Characteristics of Flooring, Floor Coverings, and Miscellaneous Materials and Assemblies” with results listed below:

    - Flame spread: 0

    - Smoke developed: 45

  - Impact Strength: Provide assembled wall protection units that have been tested in accordance with the applicable provisions of ASTM F476.

  - Chemical and stain resistance: Provide wall protection system components with chemical and stain resistance in accordance with ASTM D-1308.

  - Color match: Provide wall protection components that are color matched in accordance with the following:

    - Delta Ecmc of no greater than 1.0 using CIELab color space. (Specifier note: Construction Specialties' colors are matched under cool white fluorescent lighting and computer controlled within manufacturing tolerances. Color may vary if alternate lighting sources are present).

  - Single source responsibility: Provide all components of the wall protection system manufactured by the same company to ensure compatibility of color, texture and physical properties.

- Delivery, Storage and Handling

  - Deliver materials to the project site in unopened original factory packaging clearly labeled to show manufacturer.

  - Store materials in original, undamaged packaging in a cool, dry place out of direct sunlight and exposure to the elements. A minimum room temperature of 40°F (4°C) and a maximum of 100°F (38°C) should be maintained.

  - Material must be stored flat.

- Project Conditions

  - Materials must be acclimated in an environment of 65°-75°F (18°-24°C) for at least 24 hours prior to beginning the installation.

  - Installation areas must be enclosed and weatherproofed before installation commences.

# Part 2 - Products

- Manufacturers

  - Interior surface protection products specified herein and installed on the submittal drawings shall be manufactured by Construction Specialties, Inc.

- Materials

  - Vinyl/Acrylic: Extruded material should be high impact Acrovyn with shadowgrain grain texture, nominal .078" (1.98mm) thickness. Chemical and stain resistance should be per ASTM D-1308 standards as established by the manufacturer. Colors to be indicated in the finish schedule from one of manufacturer’s standard color range.

  - Aluminum Retainers: Extruded aluminum retainers should be 6063-T6 alloy, nominal .090" (2.29mm) thickness. Minimum strength and durability properties as specified in ASTM B221.

  - Fasteners: All fasteners to be non-corrosive and compatible with aluminum retainers. All necessary fasteners to be supplied by the manufacturer.

- Crash Rails

  - Vinyl/Acrylic crash rails to be Acrovyn by Construction Specialties: Surface, bumper or extended mounted assembly consisting of a continuous aluminum retainer or aluminum clips with snap-on Acrovyn cover and integral shock absorbing cushions. Color matched end caps and corners to be removable for ease of replacement. Attachment hardware shall be appropriate for wall conditions.

    - Model BCR-64  8" h (203.2mm) bumper mounted crash rail. Rail to be mounted with a continuous aluminum retainer with flexible cushion. Select from one of (60) Acrovyn solid colors or (16) Chameleon patterned colorways which include (14) woodgrains and (2) metals.

- Fabrication

  - General: Fabricate wall protection systems to comply with requirements indicated for design, dimensions, detail, finish and member sizes.

# Part 3 - Execution

- Examination

  - Verification of conditions: Examine areas and conditions under which work is to be performed and identify conditions detrimental to proper or timely completion.

    - Do not proceed until unsatisfactory conditions have been corrected.

- Preparation

  - Surface preparation: Prior to installation, clean substrate to remove dirt, debris and loose particles. Perform additional preparation procedures as required by manufacturer's instructions.

  - Protection: Take all necessary steps to prevent damage to material during installation as required in manufacturer’s installation instructions.

- Installation

  - Install the work of this section in strict accordance with the manufacturer's recommendations, using only approved mounting hardware, and locating all components firmly into position, level and plumb.

  - Temperature at the time of installation must be between 65°-75°F (18°-24°C) and be maintained for at least 48 hours after the installation.

  - Where splices occur in horizontal runs, splice aluminum retainer and cover at different locations along the run.

- Cleaning

  - General: Immediately upon completion of installation, clean covers and accessories in accordance with manufacturer’s recommended cleaning method.

  - Remove surplus materials, rubbish and debris resulting from installation as work progresses and upon completion of work.

- Protection

  - Protect installed materials to prevent damage by other trades. Use materials that may be easily removed without leaving residue or permanent stains.